Two-dimentional X-ray Absorption Analysis for

in Lithium Ion Battery Composite Electrode Governing Cross-sectional Reaction Distribution

Yuki Orikasa1, Yuma Gogyo2, Hisao Yamashige3, Misaki Katayama1, Kezheng Chen2, Takuya Mori2, Kentaro Yamamoto2, Titus Masese2, Yasuhiro Inada1, Toshiaki Ohta4, Zyun Siroma5, Shiro Kato6, Hajime Kinoshita6, Hajime Arai3, Zempachi Ogumi3 and Yoshiharu Uchimoto2

1) College of Life Sciences, Ritsumeikan University, Kusatsu, 525-8577, Japan

Abstract

Composite electrodes containing active materials, carbon and binder are widely used in lithium-ion batteries. Since the electrode reaction occurs preferentially in regions with lower resistance, reaction distribution can be happened within composite electrodes. We investigate the relationship between the reaction distribution with depth direction and electronic / ionic conductivity in composite electrodes with changing electrode porosities. Two dimensional X-ray absorption spectroscopy shows that the reaction distribution is happened in lower porosity electrodes. Our developed 6-probe method can measure electronic / ionic conductivity in composite electrodes. The ionic conductivity is decreased for lower porosity electrodes, which governs the reaction distribution of composite electrodes and their performances. The original manuscript was published in Sci. Rep. from the Nature Publishing Group.1 This manuscript is reprinted under a Creative Commons CC-BY license.

- Introduction

Lithium-ion batteries are promising power sources for electric vehicles, plug-in hybrid electric vehicles and so on.2 To serve these purposes, it is pivotal to improve various performance attributes of lithium-ion batteries such as capacity, safety, cyclability and high rate capability. ・・・・・・・・・・・・・・・・・・

Figure 1. Schematic illustration of a composite electrode in lithium-ion batteries.

- Experimental

The active material, carbon-coated LiFePO4 powder, with an average particle size of 200 nm was used.・・・・・・・・・・・・・・・・

- Results and Discussion

As the representative parameter, the relationship between electrode porosity and discharge capacity at 10 C rate was examined. ・・・・・・・・・・

- Conclusions

We have experimentally investigated the cross-sectional reaction distribution and the effective electronic / ionic conductivity of LiFePO4 composite electrodes with various porosities in lithium-ion batteries. ・・・・・・・・・・・・・・・・・・・・・・・・・・・

Acknowledgement

・・・・・・・・・・・・・・・・・・・・・・・・・・・・・

References

[1] Y. Orikasa, Y. Gogyo, H. Yamashige, M. Katayama, K. Z. Chen, T. Mori, K. Yamamoto, T. Masese, Y. Inada, T. Ohta, Z. Siroma, S. Kato, H. Kinoshita, H. Arai, Z. Ogumi and Y. Uchimoto, Sci. Rep., 2016, 6, 26382.

[2] M. Armand and J. M. Tarascon, Nature, 2008, 451, 652.

・・・・・・・・・・・・・・・・・・・・・・・・・・・・・

引用文献は

[数字]　著者名, 雑誌名（斜体）, 年（太字）, 巻（斜体）, 開始ページ.

に統一する。

# Text boxes

表題：

16ポイント－中央

（太文字）

著者名：

14ポイント－中央

（太文字）

12ポイントで2行　あける

12ポイントで１行　あける

所属：12ポイント－（斜体）

12ポイントで3行　あける

本文：A4・縦長・横書き

カメラレディー方式

12ポイント